# Rouse Model: Properties and Mathematical Equations

Extracted from: Rouse, P.E. Jr., J. Chem. Phys. 21(7), 1272-1280 (1953); Kuriata, A., Gront, D. & Sikorski, A., CMST 22(4), 179-185 (2016).

# 1  Static Properties

## 1.1  Gaussian Submolecule Probability

The probability that the far end of a submolecule is found at position (x, y, z) relative to its near end, assuming the submolecule is long enough for Gaussian statistics to apply.

ψ(x, y, z) dx dy dz = (β/π)^(3/2) exp[–β(x² + y² + z²)] dx dy dz

β = 3 / (2σ²),  where σ² = mean-square submolecule end-to-end separation

## 1.2  Mean-Squared End-to-End Distance

The average squared distance between the first and last beads of the chain, measuring overall chain extension.

⟨R²⟩ = ⟨(r_N – r_1)²⟩

Scaling:  ⟨R²⟩ ~ N^(2ν),   ν ≈ 0.588 (3D SAW with excluded volume)

For ideal Rouse (no excluded volume):  ⟨R²⟩ = Nσ²,  i.e. ν = 0.5

## 1.3  Mean-Squared Radius of Gyration

The average squared distance of all beads from the chain's center of mass, a less noisy measure of chain size than R².

⟨R_g²⟩ = ⟨ ∑_{i=1}^{N} (r_i – r_CM)² ⟩

Scaling:  ⟨R_g²⟩ ~ N^(2ν),   same exponent as ⟨R²⟩

## 1.4  Universal Ratio R² / R_g²

A shape diagnostic ratio that is constant for a given universality class; deviations signal sampling or equilibration problems.

⟨R²⟩ / ⟨R_g²⟩ ≈ 6.25   (3D self-avoiding walk)

Ideal chain (Gaussian):  ⟨R²⟩ / ⟨R_g²⟩ = 6

## 1.5  Configuration Probability (Full Chain)

The joint probability density for the entire chain configuration in 3N-dimensional space, assuming independent Gaussian submolecules.

Ψ = (β/π)^(3N/2) exp[–β ∑_{j=1}^{N} (x_j² + y_j² + z_j²)]

# 2  Dynamic Properties

## 2.1  Rouse Matrix Eigenvalues

Eigenvalues of the tridiagonal connectivity matrix A that couples nearest-neighbor submolecules along the chain.

λ_p = 4 sin²[ pπ / (2(N+1)) ],    p = 1, 2, …, N

## 2.2  Relaxation Times (Exact)

Each normal mode p has a characteristic relaxation time governing how quickly that mode of coordinated segmental motion decays.

τ_p = σ² / [ 24 B k T  sin²( pπ / (2(N+1)) ) ],    p = 1, 2, …, N

B = mobility of the end of a submolecule;  k = Boltzmann constant;  T = temperature

## 2.3  Relaxation Times (Long-Wavelength Approximation, p ≪ N)

For low mode numbers the sine can be approximated, yielding relaxation times independent of how the chain is subdivided.

τ_p ≈ σ² N² / (6π² p² B k T)

Equivalently using measurable quantities:
τ_p = 6(η₀ – η_s) / (π² p² n k T)

where η₀ = steady-flow solution viscosity, η_s = solvent viscosity, n = number density of polymer molecules

## 2.4  Longest Relaxation Time Scaling

The slowest mode (p = 1) sets the overall chain relaxation timescale; its scaling with N determines how simulation cost grows with chain length.

τ_R = τ_1 ~ N^(1+2ν)

Ideal Rouse (ν = 0.5):  τ_R ~ N²
With excluded volume (ν ≈ 0.588):  τ_R ~ N^2.18

## 2.5  Steady-Flow Viscosity

The zero-frequency viscosity of the polymer solution, combining the solvent contribution with the summed contributions of all relaxation modes.

η₀ = η_s + nσ² N(N+2) / (36 B)

## 2.6  Complex Viscosity Components

The real part η₁ gives the in-phase (dissipative) response and η₂ gives the out-of-phase (elastic) response under oscillatory shear.

η₁ = η_s + n k T  ∑_{p=1}^{N}  τ_p / (1 + ω² τ_p²)

η₂ = n k T  ∑_{p=1}^{N}  ω τ_p² / (1 + ω² τ_p²)

η* = η₁ – iη₂  (complex viscosity);  ω = angular frequency

## 2.7  Complex Shear Modulus Components

The storage modulus G₁ quantifies elastic energy stored per cycle and the loss modulus G₂ quantifies energy dissipated per cycle.

G* = G₁ + i G₂ = iω η*

G₁ = n k T  ∑_{p=1}^{N}  ω² τ_p² / (1 + ω² τ_p²)

G₂ = ω η_s + n k T  ∑_{p=1}^{N}  ω τ_p / (1 + ω² τ_p²)

## 2.8  High-Frequency Approximations

Closed-form expressions valid when many modes contribute, obtained by replacing the discrete mode sum with an integral.

η₁ ≈ η_s + 3(η₀ – η_s) / [π (2ωτ₁)^(1/2)],    2 < ωτ₁ < N²/250

G₁ ≈ n k T [ (π/2)(ωτ₁/2)^(1/2) – 0.5 ],    5 < ωτ₁ < N²/250

## 2.9  Diffusion Coefficient

The rate at which the chain's center of mass diffuses through the medium, inversely proportional to chain length because total friction scales linearly with N.

D = k_B T / (N ζ)

Equivalently:  D = ⟨(r(t) – r(0))²⟩ / (6t)

Scaling:  D ~ N^(–1)   (Rouse prediction)

## 2.10  Center-of-Mass Mean Square Displacement

The center of mass undergoes normal (Fickian) diffusion at all times, growing linearly with time.

g_CM(t) = ⟨(r_CM(t) – r_CM(0))²⟩ = 6 D t ~ t^1

## 2.11  Middle-Segment Mean Square Displacement

A single interior monomer shows sub-diffusive motion at short times due to chain connectivity constraints, crossing over to free diffusion once the chain has fully relaxed.

g₁(t) = ⟨(r_{N/2}(t) – r_{N/2}(0))²⟩

g₁(t) ~ t^(1/2)     for t < τ_R   (sub-diffusive, internal modes)
g₁(t) ~ t^1         for t ≥ τ_R   (free diffusion)

## 2.12  End-to-End Vector Autocorrelation

Measures how quickly the chain loses memory of its initial end-to-end orientation; the decay time defines the longest relaxation time τ_R.

g_R(t) = ⟨R(0) · R(t)⟩ / ⟨R²⟩

g_R(t) ~ exp(–t / τ_R)

τ_R extracted at g_R(τ_R) = 1/e

# 3  Model Potentials

## 3.1  Harmonic Bond (Bead-Spring / Rouse Model)

Nearest-neighbor beads are connected by harmonic springs that penalize deviations from an equilibrium bond length.

U_ij^S = k (l_ij – l₀)²

l₀ = equilibrium bond length;  k = spring constant

## 3.2  Excluded Volume (Athermal Hard-Core)

A purely repulsive step-function potential that prevents bead overlap, making the system athermal.

U_ij = E   for r_ij ≤ d_k
U_ij = 0   for r_ij > d_k

d_k = bead diameter;  E = repulsive energy barrier

# 4  Summary of Key Scaling Laws

| Property | Scaling Law | Rouse Exponent |
| --- | --- | --- |
| ⟨R²⟩, ⟨R_g²⟩ | ~ N^(2ν) | 2ν = 1.0 (ideal); ≈1.18 (SAW) |
| R² / R_g² ratio | ≈ const | 6 (ideal); ≈6.25 (SAW) |
| τ_R (longest relax.) | ~ N^(1+2ν) | 2.0 (ideal); ≈2.18 (SAW) |
| D (diffusion coeff.) | ~ N^(−1) | −1 |
| g_CM(t) | ~ t^1 | 1 |
| g₁(t), t < τ_R | ~ t^(1/2) | 0.5 |